SECTION 09 96 53

MasterProtect® EL 750 Elastomeric Coating (Formerly Thorolastic)

Notes to specifiers:

Please update your Master Specifications to reflect the company and product name changes. The old product names are provided in parentheses following the new names in this Section for reference.

The purpose of this guide specification is to assist the specifier in developing a project specification for the use of master buidlers solutions products.  this guide document has been prepared to be part of a complete project manual.  it is not intended to be a “stand alone” document, and it is not intended to be copied directly into a project manual.

This guide specification will need to be carefully reviewed for APPROPRIATENESS for the given project and edited accordingly to comply with project-specific requirements.

- GENERAL

      - SUMMARY

        - Section Includes:

          - Application of high-build, water-based, elastomeric, 100 percent acrylic, waterproof coating.

Delete sections below not relevant to this project; add others as required.

        - Related Sections:

          - Section 03 30 00 – Cast-in-Place Concrete.

          - Section 03 41 00 – Precast Structural Concrete.

          - Section 04 20 00 – Unit Masonry Assemblies.

          - Section 07 24 15 – Exterior Insulation and Finish System.

          - Section 09 24 00 – Portland Cement Plastering.

      - SUBMITTALS

        - Comply with Section [01 33 00] [__ __ __].

        - Product Data:  Submit manufacturer's technical data sheets and LEED product information for each product.

        - Submit list of project references as documented in this Specification under Quality Assurance Article.  Include contact name and phone number of person charged with oversight of each project.

        - Quality Control Submittals:

- Provide protection plan of surrounding areas and non-cementitious surfaces.

      - QUALITY ASSURANCE

        - Comply with Section [01 40 00] [__ __ __].

        - Qualifications:

          - Manufacturer Qualifications:  Company with minimum 15 years of experience in manufacturing of specified products.

          - Manufacturer Qualifications:  Company shall be ISO 9001:2000 Certified.

          - Applicator Qualifications:  Company with minimum of 5 years experience in application of specified products on projects of similar size and scope, and is acceptable to product manufacturer.

            - Successful completion of a minimum of 5 projects of similar size and complexity to specified Work.

        - Field Sample:

          - Install at Project site or pre-selected area of building an area for field sample, minimum 4 feet by 4 feet (1.2 m by 1.2 m), using specified material.

          - Apply material in accordance with manufacturer’s written application instructions.

          - Manufacturer’s representative or designated representative will review technical aspects; surface preparation, repair, and workmanship.

          - Field sample will be standard for judging workmanship on remainder of Project.

          - Maintain field sample during construction for workmanship comparison.

          - Do not alter, move, or destroy field sample until Work is completed and approved by Architect.

          - Obtain Architect’s written approval of field sample before start of material application, including approval of aesthetics, color, texture, and appearance.

          - Perform adhesion test in accordance with ASTM D3359, Method A.  Minimum adhesion rating of 4A required on 0 to 5 scale.

      - DELIVERY, STORAGE, AND HANDLING

        - Comply with Section [01 60 00] [__ __ __].

        - Comply with manufacturer’s ordering instructions and lead-time requirements to avoid construction delays.

        - Deliver materials in manufacturer's original, unopened, undamaged containers with identification labels intact.

        - Store tightly sealed materials off ground and away from moisture, direct sunlight, extreme heat, and freezing temperatures.

      - PROJECT CONDITIONS

        - Environmental Requirements:

          - Do not apply material when substrate or ambient temperature is 40 degrees F (4 degrees C) or below or is expected to fall below 40 degrees F (4 degrees C) within 24 hours after application.

          - Do not apply material if rain is expected within 24 hours of application.

          - Do not apply material to sloped (less than 60 degrees) or horizontal surfaces.

- PRODUCTS

      - MANUFACTURERs

        - Subject to compliance with requirements, provide products from the following manufacturer:

Master Builders Solutions

889 Valley Park Drive

Shakopee, MN  55379 USA

Customer Service:  800-433-9517

Technical Service:  800-243-6739

Direct Phone:  952-496-6000

Website: www.master-builders-solutions.com/en-us

        - Substitutions:  Comply with Section [01 60 00] [__ __ __].

        - Specifications and Drawings are based on manufacturer's proprietary literature from Master Builders Solutions  Other manufacturers shall comply with minimum levels of material, color selection, and detailing indicated in Specifications or on Drawings.  Architect will be sole judge of appropriateness of substitutions.

      - MATERIALS

        - High-build, water-based, elastomeric, 100 percent acrylic, waterproof coating.

          - Acceptable Product:  MasterProtect EL 750 (formerly Thorolastic) by Master Builders Solutions.

        - MasterProtect EL 750 Smooth:

          - Density, ASTM D1475:  11.2 to 12.2 lbs per gal (1.34 to 1.46 kg/L).

          - Solids Content, white, ASTM D5201:

            - By Weight:  64.2 percent.

            - By Volume:  50 percent.

          - Viscosity, ASTM D562:  127 to 135 KU.

          - VOC Content, ASTM D3960:  0.32 to 0.42 lbs per gal (38 to 50 g/L), less water and exempt solvents.

        - MasterProtect EL 750  Fine:

          - Density, ASTM D1475:  10.2 to 11.2 lbs per gal (1.22 to 1.34 kg/L).

          - Solids Content, ASTM D5201:

            - By Weight:  65.5 percent.

            - By Volume:  56 percent.

          - Viscosity, ASTM D562:  127 to 135 KU.

          - VOC Content, ASTM D3960:  0.32 to 0.42 lbs per gal (38 to 50 g/L), less water and exempt solvents.

        - MasterProtect EL 750  Coarse:

          - Density, ASTM D1475:  9.9 to 10.9 lbs per gal (1.19 to 1.31 kg/L).

          - Solids Content, ASTM D5201:

            - By Weight:  64.5 percent.

            - By Volume:  58 percent.

          - Viscosity, ASTM D562:  127 to 135 KU.

          - VOC Content, ASTM D3960:  0.32 to 0.42 lbs per gal (38 to 50 g/L), less water and exempt solvents.

        - Performance Requirements:  MasterProtect EL 750 (formerly Thorolastic Smooth), applied at 16 mils DFT:

          - Ultimate Elongation, ASTM D412:  344 percent.

          - Elongation Recovery, ASTM D412:

            - After 10 Minutes:  96.9 percent.

            - After 24 Hours:  98.4 percent.

          - Ultimate Tensile Strength, ASTM D412:  220 psi (1.5 MPa).

          - Crack Bridging, PR EN 1062-7:

            - At minus 77 degrees F (minus 60 degrees C):  12 mils (0.3 mm).

            - At 32 degrees F (0 degrees C):  19.5 mils (0.5 mm).

            - At 73 degrees F (23 degrees C):  27.5 mils (0.7 mm).

          - Flexibility, ASTM D522, at minus 30 degrees F (minus 34 degrees C):  1/8 inch (3 mm) mandrel.

          - Pull-Off Strength Adhesion, ASTM D4541:  210 psi (1.4 MPa).

          - Wind-Driven Rain, Federal Specification TT-C-555B:  Passes.

          - Water-Vapor Permeance, ASTM D1653:  10 perms.

          - Carbon-Dioxide Diffusion, PR EN 1062-6:

            - R (equivalent air-layer thickness):  263 feet (80 m).

            - Sc (equivalent concrete thickness):  8 inches (20 cm).

          - Accelerated Weathering, ASTM G23, Type D, 5,000 hours:  Passes.

          - Visual Color Change, ASTM D1729, 5,000 hours:  Passes.

          - Chalking, ASTM D4214, 5,000 hours:  Passes.

          - Freeze/Thaw Resistance, ASTM C67, 60 cycles:  Passes.

          - Salt-Spray Resistance, ASTM B117, 300 hours:  Passes.

          - Dirt Pick-Up, ASTM D3719, after 6 months exposure:  94.33 percent.

          - Mildew Resistance, ASTM D3273 and 3274:  No growth.

        - Approximate Coverage Rate:  50 to 100 sq ft per gal (4.6 to 9.3 m2/L).

        - Wet Film Thickness (WFT):

          - Smooth:  16 to 32 mils (406 to 813 microns).

          - Fine:  16 to 32 mils (406 to 813 microns).

          - Coarse:  16 to 32 mils (406 to 813 microns).

        - Dry Film Thickness (DFT):

          - Smooth:  8 to 16 mils (203 to 406 microns).

          - Fine:  9 to 18 mils (229 to 457 microns).

          - Coarse:  9 to 19 mils (229 to 483 microns).

coating is available in 4 tint bases and 48 standard colors through the elements color program.  color formulations are available through the electronic thoro tint manual.  for custom color formulations, consult master builders solutions.

        - Colors:  _______________.

delete texture below not required for project.

        - Texture:

          - Smooth.

          - Fine.

          - Coarse.

- eXECUTION

      - EXAMINATION

        - Comply with Section [01 70 00] [__ __ __].

      - SURFACE PREPARATION

        - Protection:  Protect adjacent Work areas and finish surfaces from damage during coating application.

        - Prepare surfaces in accordance with manufacturer’s instructions.

        - Ensure that substrate is sound, clean, dry, and free of dust, dirt, oils, grease, laitance, efflorescence, mildew, fungus, biological residues, and other contaminants that could prevent proper adhesion.

        - Clean surface to achieve texture similar to medium-grit sandpaper.

        - Repair holes and spalled and damaged concrete with repair materials approved by coating manufacturer.

        - Remove protruding concrete accessories and smooth out irregularities.

        - When chemical cleaners are used, neutralize compounds and fully rinse surface with clean water.  Allow surface to dry before proceeding.

        - Remove blisters or delaminated areas and sand edges to smooth rough areas and provide transition to existing paint areas.

        - Check adhesion of existing paint in accordance with ASTM D3359, measuring adhesion by Tape Method A.

        - Concrete Surfaces:

          - Cure concrete a minimum of 28 days before application.

          - Remove laitance, bond-inhibiting contaminants, form-release agents, and sealers.

          - Remove form tie wires and repair holes, small voids, and spalls using appropriate repair product approved by coating manufacturer.

          - Abrasive-blast slick, dense concrete surfaces or use primer approved by coating manufacturer.  Test surface for proper adhesion.

        - Brick and Concrete Masonry Unit (CMU) Surfaces:

          - Ensure CMUs are laid true and fully cured to full load-bearing capacity.

          - Remove mortar splatter and excess mortar.

          - Repoint or fill voids with appropriate patching product approved by coating manufacturer.

          - Ensure mortar joints are sound and free of voids and cracks.

          - Apply base coat approved by coating manufacturer to new CMUs.

        - Plaster and Stucco Surfaces:

          - Clean surfaces and remove debonded or delaminated plaster or stucco.

          - Repair with material approved by coating manufacturer.

          - Allow new plaster or stucco to cure minimum of 14 days at 70 degrees F (21 degrees C) and 50 percent relative humidity or until pH level has reached 10.  Allow longer cure times if temperatures are lower or relative humidity is higher.

          - Prime chalky surfaces with primer approved by coating manufacturer after cleaning and profiling.  Allow primer to dry.

        - Exterior Insulation and Finish System (EIFS) Surfaces:

          - Refasten or re-adhere delaminated or loose expanded polystyrene (EPS) insulation in accordance with manufacturer‘s approved methods.

          - Replace or patch missing or damaged EPS to original condition.

          - Finish with trowel acrylic finish to match and blend with existing texture.

          - Allow repaired areas to fully cure.

          - Refer to EIFS manufacturer‘s instructions for appropriate repair and procedures.

        - Existing Acrylic Coating Surfaces:

          - Sand or grind edges of existing coating to ensure adhesion and smooth transition of new material.  Sand edges of area to featheredge.

          - Wash down and allow to completely dry.

          - Prime chalky surfaces with primer approved by coating manufacturer.

        - Crack Preparation and Pretreatment:

          - Treat cracks larger than 1/32 inch (0.8 mm) and up to 1/16 inch (1.6 mm) with brush-grade acrylic crack filler approved by coating manufacturer.

          - Treat cracks larger than 1/16 by 1/16 inch (1.6 by 1.6 mm) but less than 1/4 by 1/4 inch (6 by 6 mm) with knife-grade acrylic crack filler approved by coating manufacturer.

          - Treat moving cracks larger than 1/4 by 1/4 inch (6 by 6 mm) with internally plasticized polyurethane sealant approved by coating manufacturer.

          - Apply test application of crack repair materials in inconspicuous location to ensure compatibility and aesthetic approval.

      - mixing

        - Mix coating in accordance with manufacturer’s instructions to ensure uniform color and aggregate disbursement and to minimize air entrapment.

        - In multi-pail applications, mix contents of each new pail into partially used pail to ensure color consistency and smooth transitions from pail to pail.

      - application

        - Apply coating in accordance with manufacturer’s instructions.

        - Apply coating as a 2-coat system.

        - Maintain proper uniform wet-film thickness during application to ensure performance characteristics desired.

        - Apply coating to achieve pinhole-free, consistent film build on coated surfaces.

      - Protection

        - Protect applied coating from damage during construction.

END OF SECTION

Disclaimer

THIS INFORMATION AND ALL FURTHER TECHNICAL ADVICE ARE BASED ON master builders solutions PRESENT KNOWLEDGE AND EXPERIENCE. HOWEVER, master builders solutions ASSUMES NO LIABILITY FOR PROVIDING SUCH INFORMATION AND ADVICE INCLUDING THE EXTENT TO WHICH SUCH INFORMATION AND ADVICE MAY RELATE TO EXISTING THIRD-PARTY INTELLECTUAL PROPERTY RIGHTS, ESPECIALLY PATENT RIGHTS. IN PARTICULAR, master builders solutions DISCLAIMS ALL CONDITIONS AND WARRANTIES, WHETHER EXPRESS OR IMPLIED, INCLUDING THE IMPLIED WARRANTIES OF FITNESS FOR A PARTICULAR PURPOSE OR MERCHANTABILITY. master builders solutions SHALL NOT BE RESPONSIBLE FOR CONSEQUENTIAL, INDIRECT OR INCIDENTAL DAMAGES (INCLUDING LOSS OF PROFITS) OF ANY KIND. master builders solutions RESERVES THE RIGHT TO MAKE CHANGES ACCORDING TO TECHNoLOGY PROGRESS OR FUrTHER DEVELOPMENTS. IT IS THE CUSTOMERS RESPONSIBILITY AND OBLIGATION TO CAREFULLY INSPECT AND TEST ANY INCOMING GOODS. PERForMANCE OF THE PRODUCT(S) DESCRIBED HEREIN SHOULD BE VERIFIED BY TESTING AND CARRIED OUT ONLY BY QUALIFIED EXPERTS. IT IS THE SOLE RESPONSIBILITY OF THE CUSTOMER TO CARRY OUT AND ARRANGE FOR ANY SUCH TESTING. REFERENCE TO TRADE NAMES USED BY OTHER COMPANIES IS NEITHER A RECOMMENDATION, NOR AN ENDORSeMENT OF ANY PRODUCT AND DOES NOT IMPLY THAT SIMILAR PRODUCT COULD OR COULD NOT BE USED.