SECTION MasterEmaco N 425 Repair Guide Spec

MasterEmaco N® 425 Repair Mortar (Formerly Gel Patch)

Notes to specifiers:

The Construction Systems business of BASF Corporation previously conducted business as Degussa, Inc. Building Systems.  The Admixture Systems business of BASF Corporation previously conducted business as Degussa Admixtures, Inc. and Master Builders, Inc.

On January 1, 2014 BASF launched the Master Builders Solutions brand in North America. With Master Builders Solutions, BASF combined its existing construction brands such as Master Builders, Chemrex, Sonneborn, MBT and others that have established a legacy of innovation, to create one unparalleled, globally recognized brand for its solutions to the construction industry.

This new BASF harmonized naming system, presents simpler, more logical and easier to understand product names. Each new name reflects an application property or function.

The purpose of this guide specification is to assist the specifier in developing a project specification for the use of BASF building systems’ products.  it is not intended to be a “stand alone” document, nor to be copied directly into a project manual.  This guide specification will need to be carefully reviewed for APPROPRIATENESS for the given project and edited accordingly to comply with project-specific requirements.

- GENERAL

      - SUMMARY

        - Section Includes:

          - Application of nonsag concrete repair mortar with integral corrosion inhibitor for vertical and overhead applications.

Delete sections below not relevant to this project; add others as required.

        - Related Sections:

          - Section 03 30 00 – Cast-In-Place Concrete.

          - Section 03 41 00 – Precast Structural Concrete.

          - Section 03 41 13 – Precast Concrete Hollow Core Concrete.

      - SUBMITTALS

        - Comply with Section [01 33 00] [__ __ __].

        - Product Data:  Submit manufacturer's technical data sheets and LEED product information for each product.

        - Quality Control Submittals:

          - Provide protection plan of surrounding areas and non-cementitious surfaces.

      - QUALITY ASSURANCE

        - Comply with Section [01 40 00] [__ __ __].

        - Qualifications:

          - Manufacturer Qualifications:  Company with minimum 15 years of experience in manufacturing of specified products.

          - Manufacturer Qualifications:  Company shall be ISO 9001:2000 Certified.

          - Applicator Qualifications:  Company with minimum of 5 years’ experience in application of specified products on projects of similar size and scope, and is acceptable to product manufacturer.

            - Successful completion of a minimum of 5 projects of similar size and complexity to specified Work.

        - Field Sample:

          - Install at Project site or pre-selected area of building an area for field sample, minimum 4 feet by 4 feet (1.2 m by 1.2 m), using specified material.

          - Apply material in accordance with manufacturer’s written application instructions.

          - Manufacturer’s representative or designated representative will review technical aspects; surface preparation, repair, and workmanship.

          - Field sample will be standard for judging workmanship on remainder of Project.

          - Maintain field sample during construction for workmanship comparison.

          - Do not alter, move, or destroy field sample until Work is completed and approved by Architect.

          - Obtain Architect’s written approval of field sample before start of material application, including approval of aesthetics, color, texture, and appearance.

      - DELIVERY, STORAGE, AND HANDLING

        - Comply with Section [01 60 00] [__ __ __].

        - Comply with manufacturer’s ordering instructions and lead-time requirements to avoid construction delays.

        - Deliver materials in manufacturer’s original, unopened, undamaged containers with identification labels intact.

        - Store tightly sealed materials off ground and away from moisture, direct sunlight, extreme heat, and freezing temperatures.

        - Precondition materials to 70 degrees F plus or minus 5 degrees F (21 degrees C plus or minus 3 degrees C) before mixing.

      - PROJECT CONDITIONS

        - Environmental Requirements:

          - Do not use products under conditions of precipitation or freezing weather.  Do not apply material at temperatures below 40 degrees F (4 degrees C) or above 90 degrees F (32 degrees C).  Use appropriate measures for protection and supplementary heating to ensure proper curing conditions per manufacturer's recommendations if application during inclement weather occurs.

- PRODUCTS

      - MANUFACTURERs

        - Subject to compliance with requirements, provide products from the following manufacturer:

BASF Corporation

Construction Chemicals

889 Valley Park Drive

Shakopee, MN  55379

Customer Service:  800- 433-9517

Technical Service:  800-243-6739

Direct Phone:  952-496-6000

Internet: www.master-builders-solutions.basf.us

        - Substitutions:  Comply with Section [01 60 00] [__ __ __].

        - Specifications and Drawings are based on manufacturer's proprietary literature from BASF Construction Chemicals.  Other manufacturers shall comply with minimum levels of material and detailing indicated in Specifications or on Drawings.  Architect will be sole judge of appropriateness of substitutions.

      - MATERIALS

        - Nonsag, lightweight, 1-component, high-strength, polymer-modified, silica-fume-enhanced repair mortar with integral corrosion inhibitor for vertical and overhead applications.

          - Manufactured to be placed from 1/4 inch (6 mm) to 2 inches (51 mm) per lift.

          - Acceptable Product:  MasterEmaco N 425 (formerly Gel Patch) by BASF.

        - Properties of mixed cementitious repair materials:

          - Working Time, 70 degrees F (21 degrees C):  20 to 30 minutes.

          - Color:  Concrete gray

        - Properties of cured cementitious repair materials:

          - Compressive Strength, ASTM C109, Modified:

            - 1 Day:  2,150 psi (14.8 MPa).

            - 7 Days:  5,600 psi (38.6 MPa).

            - 28 Days:  6,750 psi (46.5 MPa).

          - Splitting Tensile Strength, ASTM C496, Modified, wet cure:

            - 1 Day:  310 psi (2.1 MPa).

            - 7 Days:  560 psi (3.9 MPa).

            - 28 Days:  610 psi (4.2 MPa).

          - Flexural Strength, ASTM C348, Modified:

            - 1 Day:  500 psi (3.4 MPa).

            - 7 Days:  800 psi (5.5 MPa).

            - 28 Days:  1,110 psi (7.7 MPa).

          - Bond Strength, ASTM C882, Modified, mortar scrubbed into substrate:

            - 1 Day:  900 psi (6.2 MPa).

            - 7 Days:  1,900 psi (13.1 MPa).

            - 28 Days:   2,450 psi (16.9 MPa).

          - Chloride Permeability, AASHTO T277, ASTM C1202 Table 1:

            - Very low range.

          - Length Change, ASTM C157, wet cure:

            - 1 Day:  Plus 0.019 percent, in/in.

            - 7 Days:  Plus 0.028 percent, in/in.

            - 28 Days:  Plus 0.034 percent, in/in.

          - Length Change, ASTM C157, dry cure at 50 percent relative humidity:

            - 1 Day:  Minus 0.026 percent, in/in.

            - 7 Days:  Minus 0.11 percent, in/in.

            - 28 Days:  Minus 0.15 percent, in/in.

          - Modulus of Elasticity, ASTM C215:

            - 5.6 x 105 psi (3,861 MPa).

          - Linear Coefficient of Thermal Expansion, ASTM C531:

            - 5.3 x 10-6 in/in/degree F.

          - Water Absorption, ASTM C642:

            - 28 Days:  4 percent.

          - VOC Content:

            - 0 lbs per gal (0 g/L), less water and exempt solvents.

- EXECUTION

      - EXAMINATION

        - Comply with Section [01 70 00] [__ __ __].

      - SURFACE PREPARATION

        - Protection:  Protect adjacent Work areas and finish surfaces from damage during repair mortar application.

        - Prepare surfaces in accordance with manufacturer’s instructions.

        - Ensure surfaces are clean, sound, and free of laitance, standing water, dirt, duct, grease, oil, efflorescence, paint, curing compounds, form oils, and other surface contaminants.

        - Remove loose materials.

        - Prepare concrete substrate to fractured aggregate profile for proper adhesion.

        - Clean exposed steel reinforcement to white-metal finish and prime with anti-corrosion coating acceptable to product manufacturer.

        - Saw-cut straight edges along repair area perimeters minimum of 1/4 inch (6 mm) deep to avoid featheredges.

        - Report cracks that appear in interface area of patch or overlay to Architect, and repair as directed.

        - Continue expansion and control joints through repair or as directed by Architect.

      - mixing

        - Mix materials in accordance with manufacturer’s instructions.

        - Mix no more material than can be placed in 20 to 30 minutes at 70 degrees F (21 degrees C) and 50 percent relative humidity.

      - application

        - Apply and cure repair mortar in accordance with manufacturer’s instructions.

        - Placement:

          - Dampen surface with clean water to obtain saturated surface-dry (SSD) with no standing water.

          - Apply small quantity of mixed repair mortar to SSD substrate.  Thoroughly key-in and work material throughout cavity to promote bond.

          - Place repair mortar and key-in and compact thoroughly to secure bond.

          - Apply repair mortar in lifts of 1/4 inch (6 mm) to 2 inches (51 mm).

          - Avoid featheredging.  For optimum mechanical bond on successive lifts, thoroughly score each lift and allow reaching initial set before next layer is applied.

          - Trowel repair mortar to desired finish after initial set.

        - Curing:

          - Damp cure for 3 days.

          - Use appropriate curing compound if surface cannot be damp cured.

      - pROTECTION

        - Protect repair mortar from damage during construction.

        - Protect from freezing for minimum of 24 hours after application.

END OF SECTION

Disclaimer

This information and all further technical advice are based on BASF’s present knowledge and experience. However, BASF assumes no liability for providing such information and advice including the extent to which such information and advice may relate to existing third party intellectual property rights, especially patent rights. In particular, BASF disclaims all CONDITIONS AND WARRANTIES, WHETHER EXPRESS OR IMPLIED, INCLUDING THE IMPLIED WARRANTIES OF FITNESS FOR A PARTICULAR PURPOSE OR MERCHANTABILITY. BASF SHALL NOT BE RESPONSIBLE FOR CONSEQUENTIAL, INDIRECT OR INCIDENTAL DAMAGES (INCLUDING LOSS OF PROFITS) OF ANY KIND. BASF reserves the right to make any changes according to technological progress or further developments. It is the customer’s responsibility and obligation to carefully inspect and test any incoming goods. Performance of the product(s) described herein should be verified by testing and carried out only by qualified experts. It is the sole responsibility of the customer to carry out and arrange for any such testing. Reference to trade names used by other companies is neither a recommendation, nor an endorsement of any product and does not imply that similar products could not be used.