SECTION 03 35 16

MasterTop® 100 (Formerly Mastercron)

Notes to specifiers:

Please update your Master Specifications to reflect the company and product name changes. The old product names are provided in parentheses following the new names in this Section for reference.

The purpose of this guide specification is to assist the specifier in developing a project specification for the use of master buidlers solutions products.  this guide document has been prepared to be part of a complete project manual.  it is not intended to be a “stand alone” document, and it is not intended to be copied directly into a project manual.

This guide specification will need to be carefully reviewed for APPROPRIATENESS for the given project and edited accordingly to comply with project-specific requirements.

- GENERAL

      - SUMMARY

        - Section Includes:

          - Application of ready-to-use, colored, cementitious, mineral-aggregate, dry-shake, surface hardener.

Delete sections below not relevant to this project; add others as required.

        - Related Sections:

          - Section 03 30 00 – Cast-in-Place Concrete.

      - SUBMITTALS

        - Comply with Section [01 33 00] [ __ __ __ ].

        - Product Data:  Submit manufacturer's technical data sheets and LEED product information for each product.

        - Submit list of project references as documented in this Specification under Quality Assurance Article.  Include contact name and phone number of person charged with oversight of each project.

        - Quality Control Submittals:

          - Provide protection plan of surrounding areas and non-cementitious surfaces.

      - QUALITY ASSURANCE

        - Comply with Section [01 40 00] [ __ __ __ ].

        - Qualifications:

          - Manufacturer Qualifications:  Company with minimum 15 years of experience in manufacturing of specified products.

          - Manufacturer Qualifications:  Company shall be ISO 9001:2000 Certified.

          - Applicator Qualifications:  Company with minimum of 5 years experience in application of similar products on projects of similar size and scope, and is acceptable to product manufacturer.

            - Successful completion of a minimum of 3 projects of similar size and complexity to specified Work.

        - Field Sample:

          - Install at Project site or pre-selected area of building an area for field sample, minimum 10 feet by 10 feet (3 m by 3 m), using specified surface hardener.

          - Install with methods and equipment that will be used during slab construction.

          - Apply material in accordance with manufacturer’s written application instructions.

          - Manufacturer’s representative or designated representative will review technical aspects; surface preparation, and workmanship.

          - Field sample will be standard for judging workmanship on remainder of Project.

          - Maintain field sample during construction for workmanship comparison.

          - Do not alter, move, or destroy field sample until Work is completed and approved by Architect.

          - Obtain Architect’s written approval of field sample before start of material application, including approval of aesthetics, color, texture, and appearance.

Delete below if work of this Section is not extensive or complex enough to justify a pre-installation conference.  If retaining, coordinate with Division 1.

        - Pre-Installation Meetings:  Conduct meeting at Project site to comply with requirements in Section 01 31 00 – Project Management and Coordination.

          - Schedule and convene meeting a minimum of 1 week before starting Work of this Section.

          - Review subbase conditions, concrete mix design, weather, surface preparation, application, troweling, curing, joints, and protection.

          - Discuss procedures for protecting adjacent finished Work.

          - Provide manufacturers representative with 10 days written notice of pre-installation meeting.

      - DELIVERY, STORAGE, AND HANDLING

        - Comply with Section [01 60 00] [ __ __ __ ].

        - Comply with manufacturer’s ordering instructions and lead-time requirements to avoid construction delays.

        - Deliver materials in manufacturer's original, unopened, undamaged containers with identification labels intact.

        - Store materials in unopened packaging in clean, dry area protected from sunlight at 50 to 90 degrees F (10 to 32 degrees C).

      - PROJECT CONDITIONS

        - Environmental Requirements:

          - Do not apply over concrete containing calcium chloride or concrete containing aggregate that has been saturated with salt water.

          - Do not apply over concrete containing more than 3 percent air content as measured by ASTM C138, ASTM C173, or ASTM C231, unless approved by surface hardener manufacturer.

          - Perform Work of this Section in well-ventilated areas.

- PRODUCTS

      - MANUFACTURERs

        - Subject to compliance with requirements, provide products from the following manufacturer:

Master Builders Solutions

889 Valley Park Drive

Shakopee, MN  55379 USA

Customer Service:  800-433-9517

Technical Service:  800-243-6739

Direct Phone:  952-496-6000

Website: www.master-builders-solutions.com/en-us

        - Substitutions:  Comply with Section [01 60 00] [ __ __ __ ].

        - Specifications and Drawings are based on manufacturer's proprietary literature from Master Builders Solutions.  Other manufacturers shall comply with minimum levels of material, color selection, and detailing indicated in Specifications or on Drawings.  Architect will be sole judge of appropriateness of substitutions.

      - MATERIALS

        - Ready-to-use, colored, cementitious, mineral-aggregate, dry-shake, surface hardener to add color and improve wear resistance of concrete floors when evenly distributed and finished over freshly leveled and floated concrete.

          - Acceptable Product:  MasterTop 100 (Formerly Mastercron) by Master Builders Solutions.

          - VOC Content:  0 lbs per gal (0 g/L).

surface hardener is available in the following colors.  delete colors not required for the project.  refer to MASTER BUILDERS SOLUTIONS floor products standard color card.

        - Colors:

          - Envy.

          - High Reflective.

          - Lagoon.

          - Leather.

          - Light Reflective.

          - Mist.

          - Moondust.

          - Natural.

          - Stonewall.

          - Tomahawk.

          - Wheat.

- EXECUTION

      - EXAMINATION

        - Comply with Section [01 70 00] [ __ __ __ ].

      - Surface Preparation

        - Protection:  Protect adjacent work areas and finish surfaces from damage during surface hardener application.

        - Prepare concrete surface in accordance with manufacturer’s instructions.

contact your local MASTER BUILDERS SOLUTIONS representative for information on special suspended-slab applications.

        - Convey base concrete at maximum slump of 5 inches (127 mm) for slab on grade.

        - After concrete base has been placed, immediately screed, then bull float or highway straightedge surface.  Allow bleed water to rise to surface.

        - Monitor early moisture loss and rapid setting around perimeter of slab for proper timing of floating operation.

      - Application

        - Apply surface hardener in accordance with manufacturer’s instructions.

        - Do not apply surface hardener into bleed water.  If excessive bleed water is present, remove standing water.

        - After water sheen has disappeared and just before initial set, float surface of slab “open” with mechanical float fitted with float blades.

        - If more than 1.0 pound per square foot (4.9 kg/m2) of surface hardener will be applied, apply material in 2 or more applications.

        - Apply and float 1/2 to 2/3 of total amount of surface hardener on first application.  Apply remaining amount on subsequent applications.  Do not apply more than 1.0 pound per square foot (4.9 kg/m2) in 1 pass.

note:  Applying more than 1.0 pound per square foot (4.9 kg/m2) in 1 pass often results in limited success. In most cases, it shocks the base slab by demanding more water than is available for incorporation of the shake.  Drier areas tend to crack or delaminate, leaving less water available for subsequent shake passes.

        - Apply first application to obtain uniform distribution of surface hardener.  Where application of surface hardener will be performed by hand or square-tip shovel, apply each pass perpendicular to previous application to ensure complete coverage.

        - Float and incorporate surface hardener into surface with floating machine equipped with float blades or with wooden bull float.

note:  heavy wood float is preferable because it tends to open the slab rather than close it off, and possibly trap bleed water under surface hardener layer.

NOTE:  Do not use pan floats to incorporate the surface hardener into the base concrete, however, they may be used for final floating to achieve flatter floors.  Hand float edges with wood or laminated canvas-resin floats or darbies; magnesium floats can lead to discoloration.

        - As floating of first surface hardener application proceeds, follow immediately with subsequent material application.

        - Once second surface hardener has absorbed sufficient moisture, and surface darkens, float surface a floating machine equipped with float blades or wooden bull float.  Hand-float edges with wood floats or darbies.

        - As floating of surface hardener proceeds, follow immediately with subsequent surface hardener application, if appropriate.

      - Troweling

        - When appropriate, conduct 2 to 3 mechanical trowelings.  Leave prepared slab untouched until surface has lost its sheen and can support weight of finisher and finishing machine.  Conduct first troweling of surface.

        - On first application, keep trowel blades as flat as possible without digging into surface.

        - As surface tightens further, gradually raise trowel blades to produce desired surface.  Remove marks and pinholes in final, slightly raised trowel application.  Do not burnish colored surface hardened or light-reflective floors.

        - Only use moisture from within slab to incorporate surface hardener.  Do not apply water to aid in incorporation of surface hardener.  Under severe or rapid drying conditions, spray-apply evaporation reducer approved by surface hardener manufacturer.

        - If blistering occurs during finishing operation, flatten trowel blades immediately.  Refloat to open floor and remove blisters.  Delay raised troweling until no blisters occur.

      - Curing

        - Cure surface in accordance with manufacturer’s instructions.

        - At completion of final troweling and when surface will not be marred by foot traffic, apply membrane curing compound approved by surface hardener manufacturer.

        - Maintain ambient temperature at 50 degrees F (10 degrees C) or above during curing period.

      - Joints

        - After a minimum of 90 days, apply semi-rigid, epoxy joint filler in nonmoving control and saw-cut construction joints.  Place joint filler in accordance with joint filler manufacturer’s instructions.

        - Delay installation of joint filler as long as possible to allow slabs to adequately cure, to reduce amount of separation between slab and joint filler.

      - PROTECTION

        - After drying, protect hardened surface by covering with scuff-proof, nonstaining, builder paper.

        - Keep floors covered and free of traffic and loads for a minimum of 10 days after completion.

        - Protect completed concrete surface from damage and staining during construction.

END OF SECTION

Disclaimer

THIS INFORMATION AND ALL FURTHER TECHNICAL ADVICE ARE BASED ON master builders solutions PRESENT KNOWLEDGE AND EXPERIENCE. HOWEVER, master builders solutions ASSUMES NO LIABILITY FOR PROVIDING SUCH INFORMATION AND ADVICE INCLUDING THE EXTENT TO WHICH SUCH INFORMATION AND ADVICE MAY RELATE TO EXISTING THIRD-PARTY INTELLECTUAL PROPERTY RIGHTS, ESPECIALLY PATENT RIGHTS. IN PARTICULAR, master builders solutions DISCLAIMS ALL CONDITIONS AND WARRANTIES, WHETHER EXPRESS OR IMPLIED, INCLUDING THE IMPLIED WARRANTIES OF FITNESS FOR A PARTICULAR PURPOSE OR MERCHANTABILITY. master builders solutions SHALL NOT BE RESPONSIBLE FOR CONSEQUENTIAL, INDIRECT OR INCIDENTAL DAMAGES (INCLUDING LOSS OF PROFITS) OF ANY KIND. master builders solutions RESERVES THE RIGHT TO MAKE CHANGES ACCORDING TO TECHNoLOGY PROGRESS OR FUrTHER DEVELOPMENTS. IT IS THE CUSTOMERS RESPONSIBILITY AND OBLIGATION TO CAREFULLY INSPECT AND TEST ANY INCOMING GOODS. PERForMANCE OF THE PRODUCT(S) DESCRIBED HEREIN SHOULD BE VERIFIED BY TESTING AND CARRIED OUT ONLY BY QUALIFIED EXPERTS. IT IS THE SOLE RESPONSIBILITY OF THE CUSTOMER TO CARRY OUT AND ARRANGE FOR ANY SUCH TESTING. REFERENCE TO TRADE NAMES USED BY OTHER COMPANIES IS NEITHER A RECOMMENDATION, NOR AN ENDORSeMENT OF ANY PRODUCT AND DOES NOT IMPLY THAT SIMILAR PRODUCT COULD OR COULD NOT BE USED.