Sure Klean® Weather Seal Stone, Tile & Masonry Protector (STMP) Water Repellent Specification

Specifier Note:  The information provided below is intended to guide the Architect in developing specifications for products manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s).  The Architect should always refer to the Product Data Sheet and Safety Data Sheet for additional recommendations and for safety information

Specifier Note:  Paragraph below is for PART 1 GENERAL, Quality Assurance.

# Test Area

Test a minimum 4 ft. by 4 ft. area on each type of masonry. Use the manufacturer’s application instructions. Let test area protective treatment cure before inspection. Keep the test panels available for comparison throughout the cleaning project.

Specifier Note:  Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.

# Manufacturer

PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046.  Phone: (800) 255-4255; Fax: (785) 830-9797.  E-mail:  CustomerCare@prosoco.com

# Product Description

Sure Klean® Weather Seal Stone, Tile & Masonry Protector (STMP) is a penetrating water, oil and stain repellent. This easy-to-use, low-odor protective treatment improves stain resistance and simplifies maintenance cleaning of interior and exterior stone, quarry tile, concrete and masonry surfaces. Surfaces treated with STMP resist staining from oil, food and waterborne matter while retaining their natural color, texture and breathability.

# Typical Technical Data

FORM: Straw-colored liquid

SPECIFIC GRAVITY: 1.01

pH: 8 to 8.5

WEIGHT PER GALLON: 8.39 pounds

ACTIVE CONTENT: 3 percent

TOTAL SOLIDS: 3 percent (ASTM D 2369)

FLASH POINT: greater than 212 degrees Fahrenheit (greater than 100 degrees Celsius)

FREEZE POINT: 32 degrees Fahrenheit (0 degrees Celsius)

SHELF LIFE: 1 year in tightly sealed, unopened container

VOC: 7 grams per Liter. Complies with all known national, state and district AIM VOC regulations.

# Limitations

- Not suitable for masonry surfaces that are heavily laden with oils. Clean such surfaces with the appropriate PROSOCO cleaner before application.

- Will not compensate for structural defects or bridge cracks, gaps and voids.

- Not designed for application to asphaltic or painted surfaces.

- Do not buff or burnish treated surfaces after application.

- Not suitable for surfaces subjected to below grade water exposure.

Specifier Note:  Paragraphs below are for PART 3 EXECUTION, Installation.

# Application

Before applying, read “Preparation” and “Safety Information” sections in the Manufacturer’s Product Data Sheet for Stone, Tile & Masonry Protector (STMP).  Refer to the Product Data Sheet for additional information about application of STMP. Apply as packaged. Do not dilute or alter material. Stir or mix well before use.

Vertical Application Instructions

Apply protective treatment uniformly using enough to saturate the surface. Brush out heavy runs or drips thoroughly for uniform coverage.

Tile and Grout Sealing

Apply to grout joints using brush, roller or sponge. A second coat may be applied 1 hour later.  Avoid direct contact with water for 12 hours after material has dried. Within 24 hours of application, remove any residual haze on glazed tile by buffing with soap and water.

Horizontal Application Instructions

Apply protective treatment in a “wet-on-wet” saturating application. Sweep out puddles with a stiff bristled broom, or pick up with dry towel or mop.

Porous Surfaces

Apply in a wet-on-wet application.  Let the first application penetrate the masonry surface for 2 to 3 minutes.  Re-saturate the surface.  Less material will be required on the second application.

SPECIFIER NOTE: Extreme over application may change surface appearance.

# Drying Time

Treated surface can be opened to traffic as soon as the surface is completely dry. Protect treated surfaces from direct water contact for 12 hours. STMP gains its oil-resistant properties in 48-hours.

# Re-treatment

Periodically re-treat the surface to maintain the original performance. Apply in the same manner as the original application.

# Cleanup

Clean equipment immediate with soap and water. Remove overspray within 24-hours of application. Use mild soap and water.