GUIDE SPECIFICATION

SECTION 03360 [02760]

DRY-SHAKE COLORED HARDENER

[STAMPED/IMPRINTED CONCRETE PAVEMENT]

******************************************************************************

This guide specification is intended to be used by a qualified construction specifier.  It is not intended to be used verbatim as a project specification without appropriate modifications for the specific use intended.

Notes for review by the specifier are set off from specification text by rows of asterisks.  Optional text requiring a selection is enclosed within brackets, e.g., "Color shall be [gray] [white]."  Items requiring input specifier input are enclosed within brackets, e.g., "Color: [_______]."

******************************************************************************

- GENERAL

  - SUMMARY

    - Drawings and general provisions of Contract, including General and Supplementary Conditions and Division 1 Specification sections, apply to Work of this Section.

    - Section Includes:

      - Dry-shake colored hardener applied to [slabs-on-grade,] [sidewalks,] [driveways,] [patios,] [roads,] [parking lots,] [_______,] [and] [other exterior concrete pavements].

      - [Stamping/Imprinting.]

      - Curing of colored [and imprinted] concrete.

    - Related Sections:

      - Division 3 Section "Cast-In-Place Concrete for general applications of concrete [and for cementitious or epoxy mortar, underlayments, or toppings].

      - Division 7 Section "Joint Sealants" for colored sealants for joints.

  - REFERENCES

******************************************************************************

Other useful publications about colored concrete include:

PCA PA124 - Finishing Concrete Slabs with Color and Texture.

PCA SP021 - Color and Texture in Architectural Concrete.

******************************************************************************

    - American Concrete Institute (ACI):

      - ACI 301 "Specification for Structural Concrete for Buildings."

      - ACI 302 IR "Recommended Practice for Concrete Floor and Slab Construction."

      - ACI 303.1 "Standard Specification for Cast-In-Place Architectural Concrete."

      - ACI 304 "Recommended Practice for Measuring, Mixing, Transporting and Placing of Concrete."

      - ACI 305R "Recommended Practice for Hot Weather Concreting."

      - ACI 306R "Recommended Practice for Cold Weather Concreting."

    - American Society of Testing and Materials (ASTM):

      - ASTM C309 "Standard Specifications for Liquid Membrane-Forming Compounds for Curing Concrete."

      - ASTM C494 "Standard Specification for Chemical Admixtures for Concrete."

  - SUBMITTALS

    - Product Data:  Submit manufacturer’s complete technical data sheets for the following:

      - Dry-shake colored hardener.

      - [Powder antiquing release agent.]

      - [Imprinting/Texturing tools.]

      - Curing compound.

    - Design Mixes:  For each type of concrete.

    - Samples for Initial Selection:  Manufacturer's color charts showing full range of colors available.

    - Qualification Data:  For firms indicated in "Quality Assurance" Article, including list of completed projects.

  - QUALITY ASSURANCE

    - Manufacturer Qualifications:  Manufacturer with 10-years experience in manufacture of specified products.

    - Installer Qualifications: An installer with [5-] [________] years experience with work of similar scope and quality.

    - Comply with the requirements of ACI 301.

    - Obtain each specified material from same source and maintain high degree of consistency in workmanship throughout Project.

    - Notification of manufacturer's authorized representative shall be given at least 1-week before start of Work.

******************************************************************************

Color charts and small sample submittals provide only a general indication of color; color and appearance of completed work may differ.  On large or critical projects, specify a mock-up or field sample to demonstrate that proposed materials and workmanship produce acceptable concrete appearance.

******************************************************************************

    - Colored Concrete [Mockups] [Field Samples]:

      - Provide under provisions of Division 1 Section ["Quality Control."] [________.]

      - At location on Project selected by [Architect] [Landscape Architect] [Engineer], place and finish [10 feet by 10 feet (3 by 3 m)] [4 feet by 4 feet (1.2 by 1.2 m)] [________] area.

      - Construct [mockup][sample panel] using processes and techniques intended for use on permanent work, including curing procedures.  Include samples of control, construction, and expansion joints in sample panels.  [Mockup] [Field sample] shall be produced by the individual workers who will perform the work for the Project.

      - Accepted [mockup] [field sample] provides visual standard for work of Section.

      - [Mockup] [Field sample] shall remain through completion of the work for use as a quality standard for finished work.

      - Remove [mockup] [field sample] when directed.

  - DELIVERY, STORAGE, AND HANDLING

    - Deliver products in original factory unopened, undamaged packaging bearing identification of product, manufacturer, batch number, and expiration data as applicable.

    - Store the product in a location protected from damage, construction activity, and precipitation in strict accordance with the manufacturer's recommendations.

  - PROJECT CONDITIONS

    - Schedule placement to minimize exposure to wind and hot sun before curing materials are applied.

    - Avoid placing concrete if rain, snow, or frost is forecast within 24-hours.  Protect fresh concrete from moisture and freezing.

    - Comply with professional practices described in ACI 305R and ACI 306R.

  - PRE-JOB CONFERENCE

    - One week prior to placement of concrete, a meeting shall be held to discuss the Project and application methods.

    - It is suggested that the [Architect,] [Landscape Architect,] [Engineer,] General Contractor, [Construction Manager,] Subcontractor, Ready-Mix Concrete Representative, and a Manufacturer's Representative be present.

- PRODUCTS

  - ACCEPT ABLE MANUFACTURER

    - Sika Corporation, (800) 800-9900.

  - MATERIALS

    - Dry-shake Colored Hardener:  LITHOCHROME Color Hardener, Sika Corporation; factory proportioned, mixed, and packaged, ready-to-use surface hardener.

    - [Stamping/Imprinting Tools and Materials:]  LITHOTEX Pavecrafters imprinting tools, Sika Corporation.

    - [Powder Antiquing Release Agent:]  LITHOCHROME Antiquing Release Pro, Sika Corporation.

      - Powder antiquing release agent shall be recommended by pattern tool manufacturer and compatible with dry-shake colored hardener.******************************************************************************

Select either a curing compound in the paragraph above or a curing and sealing compound in the paragraph below.

******************************************************************************

    - Curing and Sealing Compound:  SCOFIELD Cureseal-W™ [Semi Gloss] and SCOFIELD Cureseal™ 700 [Gloss], Sika Corporation.  Curing and sealing compound shall comply with ASTM C309 and be of same manufacturer as colored admixture, for use with integrally colored concrete.

    - SUBSTITUTIONS:  The use of products other than those specified will be considered providing that Contractor requests its use in writing within 14-days prior to bid date.  This request shall be accompanied by the following:

      - A certificate of compliance from material manufacturer stating that proposed products meet or exceed requirements of this Section.

      - Documented proof that proposed materials have a 10-year proven record of performance confirmed by at least 5 local projects that [Architect] [Landscape Architect] [Engineer] can examine.

  - COLORS [AND PATTERNS]

    - Colors:  As selected by [Architect] [Landscape Architect] [Engineer] from                   Color Chart A-132CH LITHOCHROME Color Hardener.

    - [Imprinting patterns as selected by [Architect] [Landscape Architect] [Engineer] from LITHOTEX Pavecrafters™ Pattern Sheets.]

    - [Powder Antiquing Release Agent:]  As selected by [Architect] [Landscape Architect] [Engineer] from manufacturer's standard colors.

  - CONCRETE MIX DESIGN

    - Minimum Cement Content:  [5] [________] sacks per cubic yard of concrete.

    - Slump of concrete shall be consistent throughout Project at 4-inches or less.  At no time shall slump exceed 5-inches.  [If super plasticizers are allowed, slump shall not exceed 8-inches.]

    - Do not add calcium chloride to mix as it causes mottling and surface discoloration.

    - Supplemental admixtures shall not be used unless approved by manufacturer.

    - Do not add water to the mix in the field.

    - Maximum air content shall not exceed 5 percent.

- EXECUTION

  - CONCRETE PLACEMENT

    - Move concrete into place with square-tipped shovels or concrete rakes.

    - Vibrators, when used, shall be inserted and withdrawn vertically.

    - Concrete shall be struck to specified level with wood or magnesium straight edge or mechanical vibrating screed.

    - The concrete surface shall be further leveled and consolidated with highway magnesium straight edge and/or magnesium bull float.

    - Mechanically float concrete surfaces as soon as concrete surface has taken its initial set and will support weight of a power float machine equipped with float shoes or combination blades and operator.

  - INSTALLATION

    - Apply 2/3 of specified application rate to freshly floated concrete surface.  Bleed water shall not be present during or following application of first and second shake.

    - Do not throw dry-shake; distribute evenly by hand or mechanical spreader designed to apply floor hardeners. Consult Scofield for recommended manufacturers of mechanical spreaders.

    - As soon as dry-shake material has absorbed moisture, indicated by uniform darkening of surface, mechanically float concrete surface a second time, just enough to bring moisture from base slab through dry-shake color hardener.

    - Immediately following second floating, apply remaining 1/3 of specified application rate.  If applied by hand, broadcast in opposite direction of first application for a more uniform coverage.  If a mechanical spreader is used, apply the same manner as previously described.

    - As soon as dry-shake material has absorbed moisture, mechanically float concrete surface a third time.

    - Do not add water to the surface.

    - Begin imprinting operations immediately after applying dry-shake colored hardener, according to manufacturer’s written instructions, including application of powder antiquing release agent.

  - CURING

    - Imprinted concrete shall be cured with liquid membrane [curing] [curing and sealing] compound as recommended by manufacturer.

    - As soon as possible after antiquing release has been removed and after moisture content of concrete is low enough that alkali and other salts do not become trapped beneath sealer, normally a minimum of 14 to 28 days after placement, apply 2-coats of specified [sealer] [curing and sealing compound] according to manufacturer’s written instructions.

    - There should be no free water on the surface at time of application.

  - PROTECTION OF FINISHED WORK

    - Protect finish work under provisions of Division 1 Section ["Temporary Facilities and Controls."] [________.]

    - Prohibit foot or vehicular traffic on the newly imprinted concrete surface.

    - Barricade area to protect newly imprinted concrete.

    - Protect floor surface from damage until final inspection and acceptance by Owner.

******************************************************************************

Coordinate Schedule name with Drawings or delete Article if Schedule is not required.

******************************************************************************

  - SCHEDULE

    - Refer to Room Finish Schedule for locations of specified floor finish.

- 3.6	APPLICATORS

- A.	For a list of qualified contractors, contact your local Scofield representative.

END OF SECTION

© Sika Corporation